| Dr. Nuno Pessoa Barradas E-mail: nunoni@itn.pt E. N. 10, Apartado 21, 2686-953 Sacavém, PORTUGAL Tel.: +351 21 994 6150 Fax: +351 21 994 1039 The DataFurnace: http://www.ee.surrey.ac.uk/ibc/ndf/ |  |  |
| --- | --- | --- |
| REACTOR | instituto tecnológico e nuclear |  |
| Reactor | nuclear and technological institute |  |

RBS analysis of SiO2/(SiGe/SiO2) multilayer samples 12_ ag, 515, 615, 715, 815, 830 and 930 for Eliana Vieira, Universidade do Minho

#54/2010	N. P. Barradas, E. Alves, 9 de Dezembro de 2010

Samples

Samples produced in RF-sputtering technique

Schematic of structure of the multilayer samples:

SiO2 layer (1x) – 10nm

Si+Ge layer(20x) – 4nm

SiO2 layer (20x) – 10nm

p-Si substrate

The thickness of the substrate is: 256-306 µm

The annealing procedure is: RTA (Rapid thermal Annealing)

| Deposition parameters |  |  |  | Annealing conditions |  |
| --- | --- | --- | --- | --- | --- |
| Sample name | Argon pressure(mbar) | RF-Power (W) | Temperature (ºC) | Temperature (ºC) | Time (min) |
| 12_ag | 4E-03 | 80 | 350 | This sample is a as-grown sample |  |
| 12_815 |  |  |  | 800 | 15 |
| 12_715 |  |  |  | 700 | 15 |
| 12_615 |  |  |  | 600 | 15 |
| 12_515 |  |  |  | 500 | 15 |
| 12_830 |  |  |  | 800 | 30 |
| 12_930 |  |  |  | 900 | 30 |

Analysis conditions

Experiments were made 18 November (as grown) and 29 December 2010 (all other ones). Universal (large) chamber. Scattering angle 160° (standard detector for RBS)  and 28º (forward scatter ERDA detector), angle of incidence from 40º to 82º. Measurements were made at 2 MeV with 4He.

The data were analysed with the IBA DataFurnace NDF v9.3e. Please cite:

N.P. Barradas, C. Jeynes, and M.A. Harry, Nucl. Instrum. Methods Phys. Res. B136-138 (1998) 1163

Summary

The fits for all the samples are shown in the next pages. Here we try to sumarize the results.

The first comment is that in these multilayers, Si exists in all the layers. This makes it impossible to have a very accurate determination of the composition and thickness of each layer.

What we can say for sure is that in all cases a very clear multilayer structure was retained, for all the annealings done. We do not see very large changes.

The following table is based on the fits done, and we stress again that accuracy is limited by the presence of Si in all the layers. We took the average and standard deviation of the layers' thickness. We considered only the surface most layers, since the deeper ones are undistinguishable in the data. We did not include the top bilayer because it has increased H concentration. We took the 4 bilayers after the top. The H concentration quoted excludes the surface.

| sample | Ge:Si ratio | tSiGe (nm) | tSiO2 (nm) | H (at.%) |
| --- | --- | --- | --- | --- |
| AG | 30:70 | 8.0(1.3) | 6.8(1.2) | 5.1 |
| 515 | 34:66 | 7.0(1.2) | 7.7(1.2) | 1.0 |
| 615 | 34:66 | 6.4(1.2) | 7.8(1.2) | 0.7 |
| 715 | 33:67 | 6.3(1.2) | 7.2(1.2) | 1.8 |
| 815 | 34:66 | 6.5(1.2) | 6.5(1.2) | 0.5 |
| 830 | 33:67 | 6.3(1.2) | 7.5(1.2) | 0.5 |
| 930 | 35:65 | 6.1(1.1) | 7.2(1.1) | 0.15 |

The thickness values in nm were calculated assuming the bulk density of SiO2, and for the SiGe a weighted average of the atomic densities of Si and Ge. The 1H content in sample 715 is strange if we consider the trend.

Results

12_AG

The fit is:

There is H in all the film. The fitted depth profile is:

Layer  t (1e15at/cm2) t (nm) r(1e22at/cm3)     Ge        Si        O         1H

1       74.260       11.595  6.404       0.0000   30.5326   61.0651    8.4023

2       32.685        6.812  4.798      28.4481   66.5731    0.0000    4.9788

3       43.905        6.776  6.479       0.0000   31.6074   63.2148    5.1778

4       35.197        7.338  4.796      28.3457   66.3335    0.0000    5.3209

5       41.819        6.440  6.493       0.0000   31.8072   63.6144    4.5784

6       37.236        7.757  4.800      28.5419   66.7926    0.0000    4.6655

7       44.543        6.858  6.495       0.0000   31.8287   63.6574    4.5139

8       38.577        8.047  4.794      28.2133   66.0236    0.0000    5.7631

9       46.091        7.147  6.449       0.0000   31.1687   62.3374    6.4939

10       43.009        8.973  4.793      28.1621   65.9039    0.0000    5.9340

11       48.212        7.468  6.456       0.0000   31.2716   62.5432    6.1853

12       43.663        9.106  4.795      28.2566   66.1251    0.0000    5.6183

13       54.120        8.361  6.473       0.0000   31.5096   63.0192    5.4712

14       51.980       10.846  4.792      28.1240   65.8147    0.0000    6.0613

15       60.766        9.374  6.483       0.0000   31.6520   63.3041    5.0439

16       52.167       10.867  4.800      28.5573   66.8288    0.0000    4.6139

17       63.716        9.810  6.495       0.0000   31.8317   63.6633    4.5050

18       59.533       12.409  4.797      28.4020   66.4652    0.0000    5.1329

19       62.031        9.575  6.479       0.0000   31.5963   63.1927    5.2110

20       54.933       11.457  4.795      28.2602   66.1335    0.0000    5.6063

21       56.632        8.720  6.495       0.0000   31.8236   63.6472    4.5291

22       39.303        8.187  4.801      28.5906   66.9066    0.0000    4.5027

23       37.471        5.769  6.495       0.0000   31.8292   63.6585    4.5123

24       32.888        6.852  4.800      28.5136   66.7265    0.0000    4.7599

25       38.394        5.943  6.460       0.0000   31.3340   62.6681    5.9979

26       29.130        6.074  4.796      28.3141   66.2597    0.0000    5.4262

27       42.766        6.606  6.474       0.0000   31.5298   63.0595    5.4107

28       29.101        6.070  4.794      28.2208   66.0413    0.0000    5.7379

29       24.343        3.757  6.479       0.0000   31.6084   63.2168    5.1748

30       35.105        7.314  4.800      28.5279   66.7598    0.0000    4.7123

31       24.752        3.811  6.494       0.0000   31.8225   63.6449    4.5326

32       38.088        7.933  4.801      28.5892   66.9033    0.0000    4.5076

33       29.043        4.543  6.393       0.0000   36.0752   59.4115    4.5133

34       37.074        7.664  4.838      22.1254   73.3685    0.0000    4.5062

35       43.489        7.400  5.877       0.0000   57.5221   37.9733    4.5046

36       26.007        5.312  4.896      11.8162   83.6815    0.0000    4.5023

37       50.477        9.306  5.424       0.0000   76.3459   19.1508    4.5033

38       36.911        7.580  4.869      16.5588   78.9403    0.0000    4.5008

39        1.213        0.244  4.963       0.0000   95.5000    0.0000    4.5000

40    45474.914     9102.265  4.996       0.0000  100.0000    0.0000    0.0000

Total amount (1e15at/cm2):          .2026E+03 .4630E+05 .5248E+03 .8601E+02

Not considering last layer:         .2026E+03 .8273E+03 .5248E+03 .8601E+02

12_515

The fit is:

The fitted depth profile is.

Layer  t (1e15at/cm2) t (nm) r(1e22at/cm3)     Ge        Si        O         1H

1       66.132       10.253  6.450       0.0000   31.1900   62.3799    6.4301

2       31.127        6.512  4.780      32.1878   63.2587    0.0000    4.5536

3       53.780        8.235  6.530       0.0000   32.3358   64.6717    2.9925

4       35.085        7.323  4.791      32.8609   64.5816    0.0000    2.5575

5       49.651        7.609  6.525       0.0000   32.2644   64.5287    3.2069

6       32.683        6.814  4.796      33.1994   65.2469    0.0000    1.5537

7       50.533        7.687  6.573       0.0000   32.9537   65.9074    1.1389

8       31.235        6.508  4.800      33.4186   65.6777    0.0000    0.9037

9       49.245        7.485  6.579       0.0000   33.0330   66.0661    0.9009

10       34.522        7.193  4.799      33.4051   65.6511    0.0000    0.9437

11       53.394        8.116  6.579       0.0000   33.0291   66.0582    0.9127

12       38.037        7.928  4.798      33.3059   65.4561    0.0000    1.2381

13       60.049        9.132  6.576       0.0000   32.9871   65.9743    1.0386

14       39.657        8.264  4.799      33.3479   65.5387    0.0000    1.1134

15       59.115        8.994  6.573       0.0000   32.9475   65.8949    1.1576

16       44.830        9.343  4.798      33.3271   65.4979    0.0000    1.1750

17       61.687        9.378  6.578       0.0000   33.0140   66.0279    0.9581

18       39.900        8.315  4.798      33.3312   65.5059    0.0000    1.1630

19       60.566        9.207  6.578       0.0000   33.0254   66.0507    0.9239

20       41.074        8.562  4.797      33.2815   65.4081    0.0000    1.3104

21       55.022        8.372  6.572       0.0000   32.9310   65.8619    1.2071

22       33.610        7.006  4.797      33.2638   65.3735    0.0000    1.3626

23       55.259        8.408  6.572       0.0000   32.9383   65.8766    1.1852

24       35.939        7.490  4.798      33.3356   65.5146    0.0000    1.1498

25       53.371        8.114  6.578       0.0000   33.0143   66.0286    0.9572

26       34.860        7.263  4.800      33.4194   65.6793    0.0000    0.9013

27       52.415        7.967  6.579       0.0000   33.0326   66.0653    0.9021

28       33.302        6.938  4.800      33.4187   65.6778    0.0000    0.9035

29       53.754        8.171  6.579       0.0000   33.0323   66.0646    0.9031

30       33.810        7.044  4.800      33.4193   65.6790    0.0000    0.9017

31       46.869        7.124  6.579       0.0000   33.0327   66.0654    0.9019

32       34.668        7.223  4.800      33.4192   65.6787    0.0000    0.9021

33       43.015        6.722  6.399       0.0000   40.4911   58.5980    0.9109

34       31.307        6.467  4.841      26.0843   73.0081    0.0000    0.9076

35       62.020       10.656  5.820       0.0000   64.5616   34.5344    0.9040

36       28.120        5.777  4.867      21.5075   77.5909    0.0000    0.9016

37      120.636       22.449  5.374       0.0000   83.1202   15.9757    0.9041

38       29.791        6.127  4.862      22.3835   76.7162    0.0000    0.9003

39        7.799        1.224  6.372       0.0000   41.0565   57.5955    1.3480

40    41571.934     8321.044  4.996       0.0000  100.0000    0.0000    0.0000

Total amount (1e15at/cm2):          .2119E+03 .4246E+05 .6479E+03 .2556E+02

Not considering last layer:         .2119E+03 .8926E+03 .6479E+03 .2556E+02

12_615

The fit is:

The fitted depth profile is.

Layer  t (1e15at/cm2) t (nm) r(1e22at/cm3)     Ge        Si        O         1H

1       78.045       12.123  6.438       0.0000   31.0103   62.0206    6.9691

2       28.951        6.057  4.780      32.1372   63.2170    0.0000    4.6457

3       52.972        8.106  6.534       0.0000   32.3957   64.7914    2.8129

4       29.836        6.227  4.792      32.8912   64.7002    0.0000    2.4085

5       50.093        7.648  6.550       0.0000   32.6118   65.2235    2.1647

6       28.777        5.996  4.799      33.3513   65.6052    0.0000    1.0435

7       49.561        7.525  6.586       0.0000   33.1327   66.2654    0.6019

8       30.452        6.345  4.800      33.3874   65.6762    0.0000    0.9364

9       51.552        7.832  6.582       0.0000   33.0751   66.1502    0.7746

10       32.836        6.844  4.798      33.2802   65.4654    0.0000    1.2543

11       54.623        8.298  6.583       0.0000   33.0848   66.1696    0.7456

12       36.451        7.595  4.799      33.3792   65.6600    0.0000    0.9608

13       61.888        9.397  6.586       0.0000   33.1282   66.2563    0.6155

14       35.746        7.445  4.801      33.4942   65.8862    0.0000    0.6196

15       59.544        9.041  6.586       0.0000   33.1329   66.2657    0.6014

16       36.490        7.600  4.801      33.4947   65.8872    0.0000    0.6181

17       52.257        7.935  6.585       0.0000   33.1229   66.2459    0.6312

18       31.505        6.563  4.801      33.4512   65.8018    0.0000    0.7470

19       50.037        7.602  6.582       0.0000   33.0826   66.1651    0.7523

20       31.489        6.560  4.800      33.4110   65.7227    0.0000    0.8663

21       52.223        7.934  6.582       0.0000   33.0787   66.1574    0.7639

22       30.368        6.326  4.801      33.4503   65.7999    0.0000    0.7498

23       46.914        7.123  6.586       0.0000   33.1327   66.2654    0.6020

24       33.513        6.980  4.801      33.5006   65.8989    0.0000    0.6006

25       48.290        7.332  6.586       0.0000   33.1331   66.2663    0.6006

26       31.143        6.486  4.801      33.4996   65.8969    0.0000    0.6035

27       49.331        7.491  6.586       0.0000   33.1308   66.2615    0.6077

28       29.652        6.176  4.801      33.4889   65.8760    0.0000    0.6351

29       53.147        8.070  6.586       0.0000   33.1268   66.2537    0.6195

30       29.582        6.161  4.801      33.4876   65.8734    0.0000    0.6390

31       49.142        7.462  6.586       0.0000   33.1326   66.2653    0.6021

32       32.750        6.821  4.801      33.4977   65.8933    0.0000    0.6090

33       41.512        6.320  6.569       0.0000   33.6847   65.5929    0.7225

34       31.937        6.634  4.815      31.0928   68.2388    0.0000    0.6683

35       46.041        7.007  6.571       0.0000   33.5309   65.6905    0.7786

36       28.052        5.764  4.867      21.8608   77.4299    0.0000    0.7093

37       50.165        8.654  5.797       0.0000   65.6901   33.5257    0.7842

38       31.219        6.407  4.872      20.6445   78.4595    0.0000    0.8960

39       15.948        3.153  5.058       0.0000   94.1840    3.3127    2.5033

40    36375.285     7280.882  4.996       0.0000  100.0000    0.0000    0.0000

Total amount (1e15at/cm2):          .1924E+03 .3714E+05 .6396E+03 .2016E+02

Not considering last layer:         .1924E+03 .7619E+03 .6396E+03 .2016E+02

12_715

The fit is:

The fitted depth profile is.

Layer  t (1e15at/cm2) t (nm) r(1e22at/cm3)     Ge        Si        O         1H

1       72.578       11.625  6.243       0.0000   28.2304   56.4608   15.3088

2       29.025        6.067  4.784      31.1704   64.0678    0.0000    4.7618

3       49.806        7.617  6.539       0.0000   32.4581   64.9163    2.6256

4       31.185        6.514  4.788      31.3712   64.4807    0.0000    4.1480

5       47.077        7.210  6.530       0.0000   32.3254   64.6508    3.0239

6       31.630        6.602  4.791      31.5722   64.8938    0.0000    3.5340

7       45.717        6.996  6.535       0.0000   32.3960   64.7919    2.8121

8       28.660        5.977  4.795      31.7957   65.3532    0.0000    2.8511

9       45.546        6.949  6.554       0.0000   32.6776   65.3552    1.9672

10       30.307        6.313  4.800      32.1385   66.0577    0.0000    1.8039

11       43.623        6.652  6.558       0.0000   32.7308   65.4615    1.8077

12       30.121        6.275  4.800      32.1389   66.0586    0.0000    1.8025

13       49.156        7.495  6.558       0.0000   32.7333   65.4666    1.8002

14       37.255        7.761  4.800      32.1397   66.0602    0.0000    1.8002

15       60.766        9.266  6.558       0.0000   32.7333   65.4667    1.8000

16       42.963        8.950  4.800      32.1397   66.0603    0.0000    1.8000

17       65.621       10.006  6.558       0.0000   32.7333   65.4666    1.8001

18       41.993        8.748  4.800      32.1387   66.0582    0.0000    1.8031

19       62.732        9.566  6.558       0.0000   32.7332   65.4663    1.8005

20       34.475        7.182  4.800      32.1383   66.0574    0.0000    1.8043

21       52.267        7.970  6.558       0.0000   32.7333   65.4665    1.8002

22       33.054        6.886  4.800      32.1397   66.0602    0.0000    1.8001

23       51.378        7.834  6.558       0.0000   32.7333   65.4667    1.8000

24       34.002        7.083  4.800      32.1397   66.0603    0.0000    1.8000

25       48.448        7.388  6.558       0.0000   32.7333   65.4667    1.8000

26       31.285        6.517  4.800      32.1397   66.0603    0.0000    1.8000

27       45.703        6.969  6.558       0.0000   32.7333   65.4667    1.8000

28       30.466        6.347  4.800      32.1397   66.0603    0.0000    1.8000

29       54.812        8.358  6.558       0.0000   32.7333   65.4667    1.8000

30       30.084        6.267  4.800      32.1397   66.0603    0.0000    1.8000

31       44.764        6.826  6.558       0.0000   32.7333   65.4667    1.8000

32       35.548        7.405  4.800      32.1397   66.0603    0.0000    1.8000

33       33.276        5.482  6.070       0.0000   53.0292   45.1696    1.8011

34       31.691        6.544  4.843      24.6901   73.4999    0.0000    1.8101

35       55.461        8.822  6.287       0.0000   44.0186   54.1814    1.8000

36       29.378        6.047  4.859      21.9000   76.2998    0.0000    1.8002

37       52.645        8.476  6.211       0.0000   47.1313   51.0578    1.8109

38       29.731        6.113  4.863      21.0703   77.1280    0.0000    1.8017

39       15.541        3.119  4.983       0.0000   98.1939    0.0000    1.8061

40    33115.145     6628.332  4.996       0.0000  100.0000    0.0000    0.0000

Total amount (1e15at/cm2):          .1907E+03 .3389E+05 .6143E+03 .4295E+02

Not considering last layer:         .1907E+03 .7718E+03 .6143E+03 .4295E+02

12_815

The fit is:

The fitted depth profile is.

Layer  t (1e15at/cm2) t (nm) r(1e22at/cm3)     Ge        Si        O         1H

1       63.087        9.787  6.446       0.0000   31.1279   62.2558    6.6163

2       26.222        5.471  4.793      33.2452   64.8245    0.0000    1.9303

3       41.215        6.289  6.554       0.0000   32.6712   65.3424    1.9864

4       29.221        6.091  4.797      33.4958   65.3131    0.0000    1.1912

5       40.877        6.217  6.575       0.0000   32.9750   65.9500    1.0750

6       29.188        6.080  4.801      33.7258   65.7615    0.0000    0.5127

7       44.386        6.737  6.588       0.0000   33.1661   66.3322    0.5017

8       31.994        6.665  4.800      33.6806   65.6734    0.0000    0.6460

9       45.516        6.911  6.586       0.0000   33.1363   66.2727    0.5910

10       33.760        7.035  4.799      33.6199   65.5551    0.0000    0.8249

11       52.104        7.915  6.583       0.0000   33.0943   66.1886    0.7171

12       35.882        7.476  4.800      33.6546   65.6228    0.0000    0.7226

13       47.534        7.217  6.586       0.0000   33.1345   66.2690    0.5966

14       33.731        7.026  4.801      33.7229   65.7559    0.0000    0.5212

15       45.369        6.886  6.588       0.0000   33.1636   66.3272    0.5092

16       29.877        6.223  4.801      33.7298   65.7694    0.0000    0.5008

17       44.824        6.804  6.588       0.0000   33.1659   66.3317    0.5024

18       30.078        6.265  4.801      33.7280   65.7659    0.0000    0.5061

19       38.571        5.854  6.588       0.0000   33.1651   66.3303    0.5046

20       28.222        5.879  4.801      33.7241   65.7583    0.0000    0.5176

21       42.253        6.415  6.586       0.0000   33.1379   66.2758    0.5864

22       28.558        5.949  4.800      33.7029   65.7169    0.0000    0.5802

23       40.169        6.098  6.587       0.0000   33.1465   66.2931    0.5604

24       28.980        6.037  4.800      33.6853   65.6827    0.0000    0.6320

25       39.762        6.038  6.586       0.0000   33.1292   66.2584    0.6123

26       29.117        6.066  4.800      33.6786   65.6696    0.0000    0.6517

27       38.856        5.899  6.587       0.0000   33.1480   66.2959    0.5561

28       29.309        6.106  4.800      33.6731   65.6588    0.0000    0.6681

29       41.173        6.250  6.587       0.0000   33.1543   66.3086    0.5371

30       27.660        5.762  4.801      33.7249   65.7597    0.0000    0.5154

31       38.216        5.801  6.588       0.0000   33.1569   66.3138    0.5293

32       30.295        6.310  4.801      33.7251   65.7603    0.0000    0.5146

33       29.865        4.539  6.580       0.0000   33.4946   65.9859    0.5195

34       28.954        6.017  4.812      31.7398   67.7212    0.0000    0.5389

35       46.417        7.059  6.575       0.0000   33.6686   65.7953    0.5362

36       20.298        4.185  4.851      24.9394   74.5407    0.0000    0.5199

37       64.744       10.106  6.406       0.0000   40.7258   58.7646    0.5096

38       24.170        4.968  4.865      21.0372   77.3992    0.0000    1.5637

39       15.376        3.052  5.038       0.0000   93.4259    2.8530    3.7211

40    37896.059     7585.280  4.996       0.0000  100.0000    0.0000    0.0000

Total amount (1e15at/cm2):          .1816E+03 .3856E+05 .5523E+03 .1394E+02

Not considering last layer:         .1816E+03 .6680E+03 .5523E+03 .1394E+02

12_830

The fit is:

The fitted depth profile is.

Layer  t (1e15at/cm2) t (nm) r(1e22at/cm3)     Ge        Si        O         1H

1       72.510       11.307  6.413       0.0000   30.6558   61.3115    8.0327

2       30.877        6.450  4.787      31.5997   64.3839    0.0000    4.0164

3       52.141        7.961  6.550       0.0000   32.6133   65.2267    2.1600

4       30.208        6.300  4.795      32.0534   65.3083    0.0000    2.6383

5       49.212        7.523  6.542       0.0000   32.4970   64.9941    2.5089

6       29.047        6.044  4.806      32.7168   66.6600    0.0000    0.6232

7       48.449        7.353  6.589       0.0000   33.1748   66.3496    0.4757

8       29.847        6.210  4.807      32.7821   66.7931    0.0000    0.4248

9       48.006        7.284  6.591       0.0000   33.1977   66.3955    0.4068

10       31.672        6.589  4.807      32.7899   66.8090    0.0000    0.4011

11       52.704        7.997  6.591       0.0000   33.1999   66.3997    0.4004

12       35.404        7.366  4.807      32.7853   66.7995    0.0000    0.4153

13       60.730        9.220  6.587       0.0000   33.1401   66.2803    0.5796

14       37.513        7.808  4.804      32.6237   66.4702    0.0000    0.9061

15       61.807        9.384  6.587       0.0000   33.1439   66.2878    0.5684

16       36.488        7.592  4.806      32.7283   66.6835    0.0000    0.5882

17       61.623        9.350  6.591       0.0000   33.1987   66.3973    0.4040

18       33.138        6.894  4.807      32.7883   66.8057    0.0000    0.4059

19       48.790        7.403  6.591       0.0000   33.1997   66.3994    0.4009

20       30.541        6.354  4.807      32.7897   66.8085    0.0000    0.4018

21       47.536        7.213  6.591       0.0000   33.1993   66.3986    0.4021

22       28.950        6.023  4.807      32.7877   66.8045    0.0000    0.4078

23       48.418        7.351  6.587       0.0000   33.1472   66.2945    0.5583

24       28.692        5.971  4.805      32.6945   66.6146    0.0000    0.6909

25       47.811        7.258  6.587       0.0000   33.1499   66.2997    0.5504

26       30.123        6.269  4.805      32.6813   66.5876    0.0000    0.7311

27       46.633        7.079  6.588       0.0000   33.1558   66.3117    0.5325

28       29.742        6.189  4.805      32.6977   66.6210    0.0000    0.6813

29       49.679        7.540  6.588       0.0000   33.1680   66.3361    0.4959

30       28.154        5.857  4.807      32.7861   66.8013    0.0000    0.4126

31       47.784        7.250  6.591       0.0000   33.1999   66.3997    0.4004

32       29.669        6.172  4.807      32.7897   66.8086    0.0000    0.4017

33       43.534        6.609  6.587       0.0000   33.3517   66.2422    0.4061

34       31.671        6.582  4.811      31.8862   67.6300    0.0000    0.4838

35       41.881        6.356  6.589       0.0000   33.1927   66.3440    0.4632

36       25.292        5.203  4.861      22.7588   76.5152    0.0000    0.7260

37       57.211        9.262  6.177       0.0000   49.9299   49.3100    0.7601

38       25.418        5.207  4.882      18.9068   80.1368    0.0000    0.9565

39        3.082        0.549  5.613       0.0000   59.1782   29.1714   11.6503

40    33475.500     6700.460  4.996       0.0000  100.0000    0.0000    0.0000

Total amount (1e15at/cm2):          .1838E+03 .3421E+05 .6407E+03 .1753E+02

Not considering last layer:         .1838E+03 .7299E+03 .6407E+03 .1753E+02

12_930

The fit is:

The fitted depth profile is.

Layer  t (1e15at/cm2) t (nm) r(1e22at/cm3)     Ge        Si        O         1H

1       72.382       11.166  6.483       0.0000   31.6533   63.3065    5.0402

2       27.436        5.733  4.785      34.3951   63.4900    0.0000    2.1150

3       48.579        7.413  6.554       0.0000   32.6700   65.3400    1.9899

4       29.329        6.126  4.788      34.5767   63.8253    0.0000    1.5980

5       46.956        7.144  6.573       0.0000   32.9475   65.8950    1.1575

6       29.382        6.131  4.793      34.8835   64.3916    0.0000    0.7249

7       47.323        7.177  6.594       0.0000   33.2493   66.4986    0.2521

8       28.847        6.017  4.794      34.9756   64.5615    0.0000    0.4629

9       47.793        7.249  6.593       0.0000   33.2285   66.4571    0.3144

10       30.048        6.267  4.795      35.0277   64.6578    0.0000    0.3145

11       49.379        7.488  6.595       0.0000   33.2595   66.5190    0.2215

12       33.890        7.068  4.795      35.0356   64.6723    0.0000    0.2922

13       56.952        8.633  6.597       0.0000   33.2944   66.5888    0.1169

14       33.393        6.963  4.796      35.0797   64.7537    0.0000    0.1666

15       54.014        8.187  6.597       0.0000   33.2946   66.5892    0.1162

16       29.764        6.206  4.796      35.0909   64.7744    0.0000    0.1347

17       50.407        7.641  6.597       0.0000   33.2930   66.5861    0.1209

18       30.761        6.415  4.795      35.0478   64.6949    0.0000    0.2572

19       46.835        7.101  6.595       0.0000   33.2667   66.5335    0.1998

20       28.933        6.034  4.795      35.0341   64.6695    0.0000    0.2964

21       48.230        7.312  6.596       0.0000   33.2763   66.5526    0.1711

22       27.665        5.769  4.795      35.0585   64.7146    0.0000    0.2269

23       48.809        7.399  6.596       0.0000   33.2795   66.5591    0.1614

24       28.364        5.914  4.796      35.1030   64.7968    0.0000    0.1002

25       46.781        7.092  6.596       0.0000   33.2813   66.5626    0.1561

26       29.139        6.076  4.796      35.1024   64.7956    0.0000    0.1020

27       49.873        7.559  6.598       0.0000   33.2999   66.5997    0.1005

28       27.625        5.760  4.796      35.1030   64.7968    0.0000    0.1002

29       47.318        7.172  6.598       0.0000   33.3000   66.5999    0.1001

30       29.971        6.249  4.796      35.1031   64.7969    0.0000    0.1001

31       42.448        6.434  6.598       0.0000   33.3000   66.5999    0.1001

32       31.359        6.539  4.796      35.1030   64.7968    0.0000    0.1001

33       37.043        5.624  6.587       0.0000   33.7448   66.1538    0.1014

34       30.481        6.326  4.818      31.1733   68.7253    0.0000    0.1014

35       45.110        6.852  6.583       0.0000   33.8860   66.0110    0.1030

36       25.404        5.234  4.853      24.9877   74.9117    0.0000    0.1006

37       52.909        8.322  6.358       0.0000   43.2659   56.6308    0.1033

38       27.220        5.588  4.871      21.8866   78.0004    0.0000    0.1129

39       15.696        2.730  5.749       0.0000   68.1012   31.4501    0.4487

40    33364.723     6678.288  4.996       0.0000  100.0000    0.0000    0.0000

Total amount (1e15at/cm2):          .1883E+03 .3406E+05 .6211E+03 .8551E+01

Not considering last layer:         .1883E+03 .6959E+03 .6211E+03 .8551E+01